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Morris & Perry Ltd
Gurney Slade Quarry
Radstock




The above manufacturer (as represented by the undersigned) declares that the following product/s conform to the provisions of the EU Construction Products Directive, in accordance with Annex ZA of BS EN 12620, current edition.
Product description:
Carboniferous Limestone (2/6, 4/10, 4/20 & 10/20 coarse single size) Aggregates for Concrete
Coarse:		D/d ≤ 2 or D ≤ 11,2 mm and D/d > 2 or D >11,2 mm, Category GC85/20 and GC90/15

Particle shape: 			 Declared Value		Fl15 	
Particle size: 			 Designation		2/6, 4/10, 6/14, 4/20, 10/20 & 20/32mm 
							S/S Limestone	
Particle density: 		 Declared Value		2.70 Mg/m3 Typical	
Cleanliness:	Fines Quality	Pass			
Shell Content	Pass		    	SC10
Resistance to Fragmentation/						
Crushing:						LA25
Resistance to Polishing:		 			PSV37 
Resistance to Wear:					MDE15
Composition/Content:		
		Chlorides				<0.01% C
		Acid soluble sulphates			AS0.2 
		Water soluble sulphates		SS0.2 
Total sulphur				<1.0% S
		Rate of Hardening (Humus)		 Negative
		Carbonate content			>90.0% CO2
Volume stability:		Drying Shrinkage	<0.040% WS
Water Absorption:					0.70% WA
Durability against ASR:					Low Risk - Petrographic
Durability against Freeze Thaw:				MS5
 
These Aggregate products are compliant in accordance with the Assignation of Evaluation of Conformity under System 4, Table ZA.2, of BS EN 12620, current edition.

Full performance and usage applications detailed on specific[image: http://ec.europa.eu/enterprise/faq/pic/CE.png]data sheets.


Signed:						


General Manager
Issued: MARCH 2018		www.smorris.co.uk
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