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Morris & Perry Ltd
Gurney Slade Quarry
Radstock




The above manufacturer (as represented by the undersigned) declares that the following product/s conform to the provisions of the EU Construction Products Directive, in accordance with Annex ZA of BS EN 12620, current edition.
Product description:
Carboniferous Limestone 0/4mm Aggregates for Concrete

Fine:		D ≤ 4mm and d = 0, Category GF85

Particle shape: 			 Declared Value		irregular crushed rock fines 	
Particle size: 			 Designation		0/4mm S/S Limestone	
Particle density: 		 Declared Value		2.71 Mg/m3 	
Cleanliness:	Fines Quality	Pass			SE60
Shell Content	Pass		    	SC10
Resistance to Fragmentation/ Crushing: 		LANR
Resistance to Polishing:		 			PSVNR 
Resistance to Abrasion:					AAVNR
Resistance to Wear:					MDENR
Composition/Content:		
		Chlorides				<0.01% C
		Acid soluble sulphates			AS0.2
		Water soluble sulphates		SS0.2
Total sulphur				<1.0% S
		Rate of Hardening (Humus)		 Negative
		Carbonate content			>90.0% CO2
Volume stability:		Drying Shrinkage	<0.040% WS
Water Absorption:					0.70% WA
Durability against ASR:					Low Risk - Petrographic
Durability against Freeze Thaw:				MS5
These Aggregate products are compliant in accordance with the Assignation of Evaluation of Conformity under System 4, Table ZA.2, of BS EN 12620, current edition.

Full performance and usage applications detailed on specific[image: http://ec.europa.eu/enterprise/faq/pic/CE.png]data sheets.

Signed:


General Manager
Issued: MARCH 2018		www.smorris.co.uk
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