EC Declaration of Conformity

Morris & Perry Ltd

Gurney Slade Quarry

Radstock

The above manufacturer (as represented by the undersigned) declares that the following product/s conform to the provisions of the EU Construction Products Directive, in accordance with Annex ZA of BS EN 12620, current edition.

Product description:

Carboniferous Limestone 0/4mm Aggregates for Concrete

Fine:		D ≤ 4mm and d = 0, Category GF85

Particle shape: 			 Declared Value		irregular crushed rock fines

Particle size: 			 Designation		0/4mm S/S Limestone

Particle density: 		 Declared Value		2.71 Mg/m3

Cleanliness:	Fines Quality	Pass			SE60

Shell Content	Pass		    	SC10

Resistance to Fragmentation/ Crushing: 		LANR

Resistance to Polishing:		 			PSVNR

Resistance to Abrasion:					AAVNR

Resistance to Wear:					MDENR

Composition/Content:

Chlorides				<0.01% C

Acid soluble sulphates			AS0.2

Water soluble sulphates		SS0.2

Total sulphur				<1.0% S

Rate of Hardening (Humus)		 Negative

Carbonate content			>90.0% CO2

Volume stability:		Drying Shrinkage	<0.040% WS

Water Absorption:					0.70% WA

Durability against ASR:					Low Risk - Petrographic

Durability against Freeze Thaw:				MS5

These Aggregate products are compliant in accordance with the Assignation of Evaluation of Conformity under System 4, Table ZA.2, of BS EN 12620, current edition.

Full performance and usage applications detailed on specificdata sheets.

Signed:

General Manager