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BS EN 12620:2013
Aggregates for Concrete
Particle shape: 			 Declared Value		Fl15 	
Particle size: 			 Designation		4/10mm S/S Limestone	
Particle density: 		 Declared Value		2.70 Mg/m3 	
Cleanliness:	Fines Quality	Pass			
Shell Content	Pass		    	SC10
Resistance to Fragmentation/								   Crushing: 						LA25
Resistance to Polishing:		 			PSV37 
Resistance to Abrasion:					AAV15
Resistance to Wear:					MDE15
Composition/Content:		
		Chlorides				<0.01% C
		Acid soluble sulphates			AS0.2
		Water soluble sulphates		SS0.2
Total sulphur				<1.0% S
		Rate of Hardening (Humus)		 Negative
		Carbonate content			>90.0% CO2
Volume stability:		Drying Shrinkage	<0.040% WS
Water Absorption:					0.70% WA
Durability against ASR:					Low Risk - Petrographic
Durability against Freeze Thaw:				MS5
Dangerous Substances:					See Note


Note: 	Information on Dangerous Substances will only be given when and where required in the appropriate form.  Refer to BS EN 771-3:2011, Annex ZA3.
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