Morris & Perry Ltd (Gurney Slade Quarry)

Tout Quarry, Charlton Adam

Somerset        TA11 7AN

13

BS EN 12620:2013

Aggregates for Concrete

Particle shape: 			 Declared Value		Fl15

Particle size: 			 Designation		10/20mm S/S Limestone

Particle density: 		 Declared Value		2.70 Mg/m3

Cleanliness:	Fines Quality	Pass

Shell Content	Pass		    	SC10

Resistance to Fragmentation/

Crushing:						LA25

Resistance to Polishing:		 			PSV37

Resistance to Abrasion:					AAV10

Resistance to Wear:					MDE15

Composition/Content:

Chlorides				<0.01% C

Acid soluble sulphates			AS0.2

Water soluble sulphates		SS0.2

Total sulphur				<1.0% S

Rate of Hardening (Humus)		 Negative

Carbonate content			>90.0% CO2

Volume stability:		Drying Shrinkage	<0.030% WS

Water Absorption:					0.70% WA

Durability against ASR:					Low Risk - Petrographic

Durability against Freeze Thaw:				MS5

F1

Dangerous Substances:					See Note

Note: 	Information on Dangerous Substances will only be given when and where required in the appropriate form.  Refer to BS EN 771-3:2011, Annex ZA3.